# CHAPTER 76

REVISED RULES FOR CONCRETE BRIDGES

## P. Thoft-Christensen*, F.M. Jensen**, C. Middleton*** & A Blackmore***

## *Aalborg University, Aalborg, Denmark

## **CSRconsult, Aalborg, Denmark

***University of Cambridge, Cambridge, UK

Introduction

This paper is based on research performed for the Highways Agency, London, UK under the project DPU/9/44 "Revision of Bridge Assessment Rules Based on Whole Life Performance: Concrete Bridges". It contains details of a methodology which can be used to generate Whole Life (WL) reliability profiles. These WL reliability profiles may be used to establish revised rules for Concrete Bridges. The paper is to some extend based on Thoft-Christensen et al. [1] and Thoft-Christensen [2].

Limit states

Four limit states are selected for the reliability analysis:

- ultimate limit state (ULS)

(i) 	collapse limit state (using yield line analysis)

(ii  	shear failure limit state,

(b)	serviceability limit state (SLS)

(i)	crack width limit state

(ii)	deflection limit state.

## Collapse (yield line) limit state

The following safety margin (Z) is used

(1)

where V is a model uncertainty variable,  is the energy dissipated in yield lines, and  is the work done by the applied loads.

The plastic collapse analysis and estimation of the load are performed using the COBRAS program; see Middleton [3]. The reliability analysis (element and system) is done using programs RELIAB01 and RELIAB02; see [4, 5]. The RELIAB and COBRAS programs have been interfaced and include an optimisation algorithm to determine the optimal yield line pattern for each iteration of the reliability analysis, see also Thoft-Christensen [6]. The estimation of the deterioration of the steel reinforcement is based on the program CORROSION; see [7].

The basic variables used in the yield line ULS are: thickness of slab, cube strength of concrete, density of concrete, depth of reinforcement, yield strength of reinforcement, and two load parameters.

Cobras supports 16 different types of failure mode, 7 are applicable to bridge slab analysis, see figure 1.

Figure 1. Failure modes for simply supported slab bridges.

## Shear failure limit state

Shear failure is modeled using a model applicable to reinforced concrete beams (see [8]) which may be written as

(2)

where  is the shear force from external loads,  is the ultimate shear strength,  is the design shear stress, and  is the depth factor defined as, where  is the width of the beam and  is the depth of the beam

(3)

The stochastic variables used in the shear limit state are: thickness of slab, cover on reinforcement, concrete cube strength, yield stress of reinforcement, initial area of the reinforcement, density of concrete, static load factor, dynamic load factor, model uncertainty variable, and variables related to the chloride induced corrosion.

## Crack width limit state

Cracking shall be limited to a level that will not impair the proper functioning of the structure or cause its appearance to be unacceptable. In the absence of specific requirements (e.g. water tightness), it may be assumed that limitation of the maximum design crack width to about 0.3  will generally be satisfactory for reinforced concrete members  with respect to appearance and durability.

The design crack width may be obtained from (see [9])

(4)

where   is the design crack width,  is the average final spacing,  is the mean strain allowing, under the relevant combination of loads, for the effects of tension stiffening, shrinkage, etc., and  is a coefficient relating the average crack width to the design value. For load induced cracking  = 1.7. The value of  may be calculated from

(5)

where  is the stress in the reinforcement calculated on the basis of a cracked section.  is the stress in the reinforcement calculated on the basis of a cracked section under the loading conditions causing first cracking.

is a coefficient which takes account of the bond properties of the bars. It is = 1.0 for high bond bars, and = 0.5 for plain bars.  is a coefficient which takes account of the duration of the loading or of repeated loading. It is = 1.0 for single, short term loading, and = 1.5 for a sustained load or for many cycles of repeated loading.

The average final crack spacing (in mm) for members subjected dominantly to flexure or tension can be calculated from the equation

(6)

where  is the bar size in use (or the average bar size).  is the effective reinforcement ratio, , where   is the area of reinforcement contained within the effective tension area, .  is a coefficient which takes account of the bond properties of the bar. It is = 0.8 for high bond bars and = 1.6 for plain bond bars.  is a coefficient which takes account of the strain distribution. It is = 0.5 for bending and = 1.0 for pure tension.

The crack width limit state can then be formulated by

(7)

where  is a model uncertainty stochastic variable.

The stochastic variables used in the crack SLS are: concrete cover, distance between reinforcement bars, diameter of reinforcement bars, thickness of slab, elastic modulus of reinforcement bars, tensile strength of concrete, external bending moment, and one model uncertainty variable.

## Deflection limit state

The following limit state is used

(8)

Where dmax is the maximum allowable deflection; dk is the defection estimated by linear analysis, and zd is a model uncertainty variable.

Deterioration

Mathematical modeling

Several models can be used to model the deterioration of reinforcement steel in concrete slabs. However, there is a general agreement that the model presented below is acceptable in most cases.

Corrosion initiation period refers to the time during which the passivation of steel is destroyed and the reinforcement starts to corrode actively. Practical experience of bridges in wetter countries like UK shows that chloride ingress is far bigger a problem that carbonation.

The rate of chloride penetration into concrete, as a function of depth from the concrete surface and time, can   be represented by Fick's law of diffusion as follows:

(9)

where  is the chloride ion concentration, as % of the weight of cement, at distance  cm from the concrete surface after  seconds of exposure to the chloride source.  is the chloride diffusion coefficient expressed in cm2/sec. The solution of the differential equation (9) is

(10)

where  is the equilibrium chloride concentration on the concrete surface, as % of the weight of cement,  is the distance from the concrete surface in cm,  is the time in sec, erf is the error function,  is the diffusion coefficient in cm2/sec and  is the chloride concentration at any position  at time . In a real structure, if  is assumed to be the chloride corrosion threshold and  is the thickness of concrete cover, then the corrosion initiation period,, can be calculated based on a knowledge of the parameters  and . For bridge decks under de-icing conditions =1.6, as % of cement weight, is often used.

The time  to initiation of reinforcement corrosion is

(11)

where  is the initial chloride concentration,  is the critical chloride concentration at which corrosion starts, and  is the concrete cover. For plain concrete of moderate strength () reported values of  are in the range between  and .

When corrosion has started then the diameter  of the reinforcement bars at time t is modeled by

(12)

where  is the initial diameter,  is a corrosion coefficient, and   is the rate of corrosion. The area of a reinforcement bar is then modeled using the following formulation

(12)

where

,

A(t) is the area of reinforcement bars  at the time t years, n is the number of reinforcement bars,  is the diameter of a single bar  and  is the corrosion initiation time in years. The value "0.0203" in the estimation of  will vary depending on the circumstances.

The initiation time of corrosion is determined based on values of . After the deterioration is started the corrosion rate is modeled by the corrosion current  only.

The model for  (and the value of  used) relates to an average deterioration of the reinforcement in the concrete. An important aspect of corrosion in addition to the average corrosion is the maximum penetration (pitting of reinforcement). Pitting of reinforcement may have more influence on the reliability than the average deterioration due to localised much higher weakening of the reinforcement. The ratio  between the maximum penetration  and the average penetration  has been estimated by a number of authors to be between 4-10; see e.g. González et al. [10]. Pitting corrosion is not included in this investigation.

The stochastic variables used in the deterioration modeling are: initial chloride concentration on surface, initial chloride concentration in concrete, diffusion coefficient for the concrete, cover to reinforcement, critical chloride concentration, and rate of corrosion.

Based on a survey the following modeling for chloride penetration is proposed (the initial chloride is assumed to be zero):

Model 0:	Diffusion coefficient  			: 	N(30.0, 5.0) [mm2/year]

Chloride concentration, surface 	 : 	N(0.65, 0.075) [%]

Corrosion density 			: 	Uniform[1.0,3.0] [A/cm2]

(Cover on reinforcement 		: 	N(40.0, 4.0) [mm])

Figure 2 shows sample realizations of the chloride concentrations (at the depth of the reinforcement bar) for Model 0. Figure 3 shows sample realizations of the deterioration history of the reinforcement area for the same model.

Based on the deterioration model 0 three levels of deterioration are proposed: low deterioration, medium deterioration and high deterioration. The deterioration parameters for these three levels are:

Low:		Diffusion coefficient  		: 	N(25.0, 2.5) [mm2/year]

Chloride concentration, surface 	 : 	N(0.575, 0.038) [%]

Corrosion density 			: 	Uniform[1.0, 2.0]  [mA/cm2]

Medium:	Diffusion coefficient 	 	: 	N(30.0, 2.5) [mm2/year]

Chloride concentration, surface 	 : 	N(0.650, 0.038) [%]

Corrosion density 			: 	Uniform[1.5, 2.5]  [mA/cm2]

High:	Diffusion coefficient  		: 	N(35.0, 2.5) [mm2/year]

Chloride concentration, surface 	 : 	N(0.725, 0.038) [%]

Corrosion density		 	: 	Uniform[2.0, 3.0]  [mA/cm2]

Figure 4 shows sample realizations for the chloride concentration (at the depth of the reinforcement bar) for deterioration models: low, medium, high. The profiles obtained using mean values are shown for all three models. Figure 5 shows the sample realizations of the history of the reinforcement area for deterioration models: low, medium, high. The profiles obtained using mean values are shown for all three models.

Reliability profiles

This following example is used to illustrate the proposed methodology. The example is based on an existing UK bridge, but some limitations and simplifications are made. The bridge was built in 1975.

Figure 6. Bridge data.

| Stochastic variables: Yield line limit state |
| --- |
| No | Type | Par. 1 | Par. 2 | Description |
| 1 | Normal | 550.0 | 10.0 | Thickness of slab [mm] |
| 2 | LogNormal | 30.0 | 6.0 | Cube strength of concrete [MPa] |
| 3 | Normal | 23.6 | 0.4 | Density of concrete [kN/m3] |
| 4 | LogNormal | 289.0 | 25.0 | Yield strength: longitudinal reinforcement [MPa] |
| 5 | Normal | 60.0 | 8.0 | Cover on longitudinal reinforcement [mm] |
| 6 | LogNormal | 289.0 | 25.0 | Yield strength: transverse reinforcement [MPa] |
| 7 | Normal | 86.0 | 8.0 | Cover on transverse reinforcement [mm] |
| 8 | Fixed | 10053.0 | - | Longitudinal reinforcement area (initial) [mm2] |
| 9 | Fixed | 565.0 | - | Transverse reinforcement area (initial) [mm2] |
| 10 | Gumbel | 0.352 | 0.026 | Static load factor [-] |
| 11 | Normal | 1.27 | 0.20 | Dynamic load factor [-] |
| 12 | Normal | 1.08 | 0.072 | Chloride concentration on surface [%] |
| 13 | Fixed | 0.0 | - | Initial chloride concentration [%] |
| 14 | Normal | 35.0 | 2.5 | Diffusion Coefficient [cm2/sec] |
| 15 | Normal | 0.4 | 0.05 | Critical Chloride concentration [%] |
| 16 | Uniform | 2.5 | 0.29 | Corrosion parameter [-] |
| 17 | Normal | 1.0 | 0.05 | Model uncertainty variable [-] |

Table 1. Stochastic modeling used for the ULS.

The bridge was designed for 45 units HB load, see [10]. The bridge has a span of 9.755 m, the width is 213.71 m, and the slab thickness is 550 mm (see figure 6).

Based on the corrosion data shown in table 1 the expected area of the reinforcement as a function of time can be calculated, see figure 7.

Reliability profiles for the limit states discussed in section 2 are calculated on the basis of the stochastic modeling shown in tables 1 and 2.

| Stochastic variables: Crack width limit state |
| --- |
| No | Type | Par. 1 | Par. 2 | Description |
| 1 | Normal | 60.0 | 9.0 | Concrete cover [mm] |
| 2 | Normal | 125.0 | 12.5 | Distance between reinforcement bars [mm] |
| 3 | Normal | 40.0 | 1.2 | Diameter of reinforcement bar [mm] |
| 4 | Normal | 550.0 | 27.0 | Thickness of slab [mm] |
| 5 | Normal | 200.0E3 | 6.0E3 | Young's modulus [N/mm2] |
| 6 | Normal | 3.4 | 0.68 | Tensile strength [N/mm2] |
| 7 | Gumbel | 1.0 | 0.10 | Model uncertainty [-] |
| 8 | Gumbel | 0.352 | 0.026 | Static load factor [-] |
| 9 | Normal | 1.27 | 0.20 | Dynamic load factor [-] |
| 10 | Normal | 1.08 | 0.072 | Chloride concentration on surface [%] |
| 11 | Fixed | 0.0 | - | Initial chloride concentration [%] |
| 12 | Normal | 35.0 | 2.5 | Diffusion Coefficient [cm2/sec] |
| 13 | Normal | 0.4 | 0.05 | Critical Chloride concentration [%] |
| 14 | Uniform | 2.5 | 0.29 | Corrosion parameters [-] |

Table 2. Stochastic modeling used for the SLS.

The general traffic highway load model in the Eurocode 1, Part 3 (ENV 1991-3:1995) for lane and axle load is applied. The load effects produced by the Eurocode model (lane and axle load) are multiplied by a static load factor (extreme type 1) and a dynamic load factor (normal).

The normalized reliability profile for the yield line ULS (full width failure) and the corresponding probability of failure profile are shown in figure 8.  The reliability index at time t = 0 is =11.5.  Due to the size of the concrete cover (mean value 60 mm) the deterioration does not have any effect until year 70.

The results from the sensitivity analysis with regard to the mean values are shown for t = 0 years and t = 120 years in figure 9. The most important variables are, as expected, the thickness of the slab, the yield strength of the reinforcement, and the model uncertainty. Observe that the magnitude of sensitivity with regard to the cover changes from negative at time t = 0 years to positive at time t = 120 years due to the corrosion.

The normalized reliability profile for the crack SLS and the corresponding probability of failure profile are shown in figure 10. The reliability index at time t = 0 is =7.1. Due to the size of the concrete cover (mean value 60 mm) the deterioration does not have any effect until year 90.

The results from the sensitivity analysis with regard to the mean values are shown for t = 0 years and t = 120 years in figure 11. The most important variables are as expected the concrete cover, the diameter of the reinforcement, the thickness of the slab, and Young's modulus. Observe that the magnitude of the sensitivity with regard to the cover is decreasing from time t = 0 years to time t =120 years due to the corrosion.

K  factor profiles

In this section a new procedure is proposed for use by engineers when assessing bridges.

For a given bridge, using the loading given in the Assessment Code BD 21, the available load capacity factor K is initially calculated. A chart like figure 12 is supplied to the assessing engineer. If the calculated K factor is below the indicated safety level then immediate action is required (e.g. strengthening, repair, or replacement).

If the load capacity factor K is above the lines (b), (c), or (d) corresponding to the road being a trunk road, a principal road or a minor road, or line (e) (shown schematically in figure 12), then the bridge can be deemed satisfactory and no strengthening work is needed at present.

If the load capacity factor K is within the intermediate zone (the safety line and lines (b), (c), (d) or (e)), the assessing engineer is required to determine all reasonable alternative strengthening/maintenance strategies for the bridge. These data and alternatives are then made available to the owner/maintainer of the bridge who then decides which actions to take.

Acknowledgement

The authors would like to thank the Highways Agency, London for permission to publish this paper. The work herein was carried out under a contract placed on CSRconsult by the HA. The authors are particularly grateful to Dr. P. Das of the Highways Agency for his contributions to the fundamental philosophy of this work. However, any views expressed in this paper are not necessarily those of the Highways Agency of the U.K. Department of Transport.

References

- Thoft-Christensen, P., F.M. Jensen, C. Middleton & A. Blackmore: “Assessment of the Reliability of Concrete Slab Bridges”. Proceedings IFIP WG7.5 Conference, Boulder, USA, April 2-4, 1996, 321-328.

- Thoft-Christensen, P: “Re-Assessment of Concrete Bridges”. ASCE Structures 	Congress, Chicago, USA, April 14-18, 1996

- Middleton, C. Example Collapse & Reliability Analyses of Concrete Bridges 	using a new Analyses Technique. Cambridge University, 1994.

- RELIAB01, Version 2.0, manual and software. CSR-software, March 1994.

- RELIAB02, Version 2.0, manual and software. CSR-software, April 1994.

- P. Thoft-Christensen: “Reliability of Plastic Slabs”, ICOSSAR Conference, 	San 	Francisco, USA, August 1989.

- CORROSION, Version 1.0, manual and software. CSR-software, September 	1995.

- Imperial College (1995). “Reliability Calibration of Short Span Bridge Load Model”. Department of Civil Engineering, Imperial College.

- Eurocode 2: Design of concrete structures - Part 1-1: General rules and rules 	for buildings, ENV 1992-1:1991.

- J .A. González, C. Andrade, C. Alonso & S. Feliu: "Comparison of Rates of 	General Corrosion and Maximum Pitting Penetration on Concrete Embedded 	Steel Reinforcement", Cement and Concrete Research, Vol. 25, No. 2, pp. 	257-264, 1995.

- Department of Transport. Loads for Highway Bridges. Departmental Standard 	BD37/88, London, 1989.

# Footnotes

Symposium on “Safety of Bridges”, London, UK, July 1996. In “Safety of Bridges” (ed. P.C. Das), Highways Agency, 1996, pp. 175-188.

# Text boxes

Figure 12. Typical form of load capacity factor chart.

Figure 10: Reliability profiles using a crack width limit state.

Figure 9: Sensitivity analysis for yield line limit state at t = 0 years and at t = 120 years.

Figure 11: Sensitivity analysis for crack width limit state at t = 0 years

and at t = 120 years.

Figur 8. : Reliability profiles using a yield line limit state.

Figure 7. Reinforcement area A(t) as a

function of time.

Figure 5. Normalized reinforcement area  as a function

of time for low, medium, and high deterioration.

Figure 4. Samples showing the chloride concentration as

a function of time for low, medium and high deterioration.

Figure 3. Normalized reinforcement area  as a function of time for Model 0.

Figure 2. Samples showing the chloride concentration

as a function of time for Model 0.