# CHAPTER 79

RELIABILITY PROFILES FOR CONCRETE BRIDGES

P. Thoft-Christensen

University of Aalborg, Denmark.

### ABSTRACT

In this paper calculation of reliability profiles is discussed. ULS as well as SLS limit states are formulated. Corrosion due to chloride penetration is the considered deterioration mechanism. Three models for corrosion are formulated. The proposed method for calculating reliability profiles is illustrated on an existing UK bridge.

INTRODUCTION

This paper is based on research performed for the Highways Agency, London, UK under the project DPU/9/44 “Revision of Bridge Assessment Rules Based on Whole Life Performance: Concrete Bridges”. It contains details of a methodology which can be used to generate Whole Life (WL) reliability profiles. These WL reliability profiles may be used to establish revised rules for Concrete Bridges. The paper is based on Thoft-Christensen et al. [1], Thoft-Christensen et al. [2], and Thoft-Christensen [3].

LIMIT STATES

Four  limit states are selected for the reliability analysis:

- two ultimate limit states (ULS):     collapse limit state (using yield line analysis) 			                              shear failure limit state,

- two serviceability limit states (SLS):  crack width limit state

deflection limit state.

Collapse (yield line) limit state

The following safety margin is used

M1=Z1ED−WD                                	                    (1)

- where Z1 is a model uncertainty variable, ED is the energy dissipated in yield lines, and WD is the work done by the applied loads.

The plastic collapse analysis and estimation of the load are performed using the COBRAS programme; Middleton [4]. The reliability analysis (element and system) is done using RELIAB01 [5] and RELIAB02 [6]. The RELIAB and COBRAS programmes have been interfaced and an optimisation algorithm has been included to determine the optimal yield line pattern for each iteration of the reliability analysis, see also Thoft-Christensen [7]. The estimation of the deterioration of the steel reinforcement is based on the programme CORROSION [8].  The basic variables used in the yield line ULS are: thickness of slab, cube strength of concrete, density of concrete, depth of reinforcement, yield strength of reinforcement, and two load parameters.

Shear failure limit state

Shear failure is modelled using a model applicable to reinforced concrete beams; see Imperial College [9], which may be written as

(2)

where Vj is the shear force from external loads,  is the ultimate shear strength , and Z2  is an model uncertainty variable.

The stochastic variables used for the shear limit state are: thickness of slab, cover of reinforcement, concrete cube strength, yield stress of reinforcement, initial area of the reinforcement, density of concrete, static load factor, dynamic load factor, model uncertainty variable, and variables related to the chloride induced corrosion.

## Crack width limit state

Cracking shall be limited to a level that will not impair the proper functioning of the structure or cause its appearance to be unacceptable. The design crack width may be obtained from; see Eurocode [10]

(3)

where  Wk is the design crack width, srm is the average final spacing, esm is the mean strain, under the relevant combination of loads, allowing for the effects of tension stiffening, shrinkage, etc., and b is a coefficient relating the average crack width to the design value.  The value of εsm may be calculated from

εsm=σsEs(1−β1β2(σsrσs)2)                                              (4)

where  is the stress in the reinforcement calculated on the basis of a cracked section.  is the stress in the reinforcement calculated on the basis of a cracked section under the loading conditions causing first cracking. β1 is a coefficient which takes account of the bond properties of the bars.

The average final crack spacing (in mm) for members subjected dominantly to flexure or tension can be calculated from the equation

srm=50+0.25k1k2φρr                                                  (5)

where  is the bar size in use (or the average bar size). ρr is the effective reinforcement ratio, AsAc.eff, where  As is the area of reinforcement contained within the effective tensile area, Ac.eff. k1 and k2  are coefficients taking account of the bond properties of the bar and the strain distribution, respectively.

The crack width safety margin can then be formulated by

(6)

where Z3 is a model uncertainty stochastic variable. The stochastic variables used in the crack SLS are: concrete cover, distance between reinforcement bars, diameter of reinforcement bars, thickness of slab, elastic modulus of reinforcement bars, tensile strength of concrete, external bending moment, and one model uncertainty variable.

## Deflection limit state

The following deflection safety margin is used

M4=Dmax−Z4D                                                          (7)

where Dmax is the maximum allowable deflection, D is the deflection estimated by linear elastic analysis, and Z4 is a model uncertainty variable.

DETERIORATION

Corrosion initiation period refers to the time during which the passivation of steel is destroyed and the reinforcement starts to corrode actively. Practical experience of bridges in wetter countries shows that chloride ingress is a far bigger problem than carbonation. The rate of chloride penetration into concrete, as a function of depth from the concrete surface and time, can be represented by Fick's law of diffusion as follows:

(8)

where C(x,t) is the chloride ion concentration, as % by weight of cement, at a distance of x cm from the concrete surface after t seconds of exposure to the chloride source. DC is the chloride diffusion coefficient expressed in cm2/sec. The solution of the differential equation (8) is

C(x,t)=C01−erfx2DC⋅t                                           (9)

where C0 is the equilibrium chloride concentration on the concrete surface, as % of the weight of cement, x is the distance from the concrete surface in cm, t is the time in sec, erf is the error function, DC is the diffusion coefficient in cm2/sec and C(x,t) is the chloride concentration at any position x at the time t. In a real structure, if Ccr is assumed to be the chloride corrosion threshold and d−D2 is the thickness of concrete cover, then the corrosion initiation period, , can be calculated.  The time TI to initiation of reinforcement corrosion is

TI=(d−D2)24DC(erf−1(Ccr−C0Ci−C0))−2                                     (10)

When corrosion has started the diameter D(t) of the reinforcement bars at the time t is modelled by

D(t)=D−CCorricorrt                                                (11)

Figure 1. Normalized reinforcement area 
 as a function of time

for low, medium, and high deterioration.

where D1 is the initial diameter, Ccorr is a corrosion coefficient, and icorr  is the rate of corrosion.

Based on a survey, three models for chloride penetration are proposed (the initial chloride is assumed to be zero): low deterioration, medium deterioration and high deterioration. The deterioration parameters for these three levels are:

Low:	Diffusion coefficient  		DC: 	N(25.0, 2.5) [mm2/year]

Chloride concentration, surface 	C0 : 	N(0.575, 0.038) [%]

Corrosion density 	icorr: 	Uniform[1.0, 2.0]  [mA/cm2]

Medium:	Diffusion coefficient 	 		DC: 	N(30.0, 2.5) [mm2/year]

Chloride concentration, surface 	C0 : 	N(0.650, 0.038) [%]

Corrosion density 	  icorr: 	Uniform[1.5, 2.5]  [mA/cm2]

High:	Diffusion coefficient  		DC: 	N(35.0, 2.5) [mm2/year]

Chloride concentration, surface 	C0 : 	N(0.725, 0.038) [%]

Corrosion density	icorr: 	Uniform[2.0, 3.0]  [mA/cm2]

Figure 1 shows sample realizations of the history of the reinforcement area for all tree deterioration models.

Reliability profiles

Figure 2. Bridge data.

This example is used to illustrate the proposed methodology. The example is based on an existing UK bridge, but some limitations and simplifications are made. The bridge was built in 1975.

The bridge was designed for 45 units HB load. The bridge has a span of 9.755 m, the width is 213.71 m, and the slab thickness is 550 mm (see figure 2). Based on the corrosion data shown in table 1 the expected area of the reinforcement can be calculated as a function of time, see figure 3

Figure 3. Expected reinforcement area E[A(t)] as a function of time.

.

Reliability profiles for the yield line limit state (ULS) are, as an illustration, calculated on the basis of the stochastic modelling shown in table 1.

The general traffic highway load model in the Eurocode 1, Part 3 (ENV 1991-3:1995) for lane and axle load is applied. The load effects produced by the Eurocode model (lane and axle load) are multiplied by a static load factor (extreme type 1) and a dynamic load factor (normal).

The normalized reliability profile for the yield line ULS (full width failure) and the corresponding probability of failure profile are shown in figure 4.  The reliability index at the time t = 0 year is β0=11.5.  Due to the size of the concrete cover (mean value 60 mm) the deterioration does not have any effect until year 70.

| Stochastic variables: Yield line limit state |  |  |  |  |
| --- | --- | --- | --- | --- |
| No | Type | Par. 1 | Par. 2 | Description |
| 1 | Normal | 550.0 | 10.0 | Thickness of slab [mm] |
| 2 | LogNormal | 30.0 | 6.0 | Cube strength of concrete [MPa] |
| 3 | Normal | 23.6 | 0.4 | Density of concrete [kN/m3] |
| 4 | LogNormal | 289.0 | 25.0 | Yield strength: longitudinal reinforcement [MPa] |
| 5 | Normal | 60.0 | 8.0 | Cover on longitudinal reinforcement [mm] |
| 6 | LogNormal | 289.0 | 25.0 | Yield strength: transverse reinforcement [MPa] |
| 7 | Normal | 86.0 | 8.0 | Cover on transverse reinforcement [mm] |
| 8 | Fixed | 10053.0 | - | Longitudinal reinforcement area (initial) [mm2] |
| 9 | Fixed | 565.0 | - | Transverse reinforcement area (initial) [mm2] |
| 10 | Gumbel | 0.352 | 0.026 | Static load factor [-] |
| 11 | Normal | 1.27 | 0.20 | Dynamic load factor [-] |
| 12 | Normal | 1.08 | 0.072 | Chloride concentration on surface [%] |
| 13 | Fixed | 0.0 | - | Initial chloride concentration [%] |
| 14 | Normal | 35.0 | 2.5 | Diffusion Coefficient [cm2/sec] |
| 15 | Normal | 0.4 | 0.05 | Critical Chloride concentration [%] |
| 16 | Uniform | 2.5 | 0.29 | Corrosion parameter [-] |
| 17 | Normal | 1.0 | 0.05 | Model uncertainty variable [-] |

Table 1. Stochastic modelling used for the ULS.

Figure 4. : Reliability profiles using a yield line limit state.

The results from the sensitivity analysis with regard to the mean values are for illustration shown for t = 0 years and t = 120 years in figure 5. 17 stochastic variables are used in this reliability assessment and the corresponding elasticities are shown in figure 5. The most important variables are, as expected, the thickness of the slab, the yield strength of the reinforcement, and the model uncertainty. Observe that the magnitude of sensitivity with regard to the cover changes from negative at the time t = 0 years to positive at time t = 120 years due to the corrosion.

Figure 5: Sensitivity analysis for yield line limit state at t = 0 years and at t = 120 years.

Acknowledgement

The author would like to thank the Highways Agency, London, for permission to publish this paper. The work herein was carried out under a contract placed with CSRconsult by the HA. The author is particularly grateful to Dr. P. Das of the Highways Agency for his contributions to the fundamental philosophy of this work. However, any views expressed in this paper are not necessarily those of the Highways Agency of the U.K. Department of Transport.

The author would also like to thank Dr. C. Middleton and Dr. A. Blackmore, Cambridge University, UK and Dr. F.M. Jensen, CSRconsult, Aalborg, Denmark, for their significant contributions to the research presented in this paper.

References

[1]  	Thoft-Christensen, P., C. Middleton & A. Blackmore: “Revised Rules for Concrete Bridges”, Symposium on the Safety of Bridges, London, July 4-5, 1996.

[2]  	Thoft-Christensen, P., F.M. Jensen, C. Middleton & A. Blackmore: "Assessment of the Reliability of Concrete Slab Bridges", IFIP WG7.5 Conference, Boulder, USA, April 2-4, 1996.

[3] 	Thoft-Christensen, P: “Re-Assessment of Concrete Bridges”, ASCE  Structures 	Congress, Chicago, USA, April 14-18, 1996.

[4]   	Middleton, C. “Example Collapse & Reliability Analyses of Concrete Bridges Using a new Analyses Technique”, Cambridge University, 1994.

[5]    	RELIAB01, Version 2.0, manual and software. CSR-software, March 1994.

[6]    	RELIAB02, Version 2.0, manual and software. CSR-software, April 1994.

[7]  	Thoft-Christensen, P.: “Reliability of Plastic Slabs”, ICOSSAR Conference, San Francisco, USA, August 1989.

[8]   	CORROSION, Version 1.0, manual and software. CSR-software, September 1995.

[9]  	Imperial College: "Reliability Calibration of Short Span Bridge Load Model", 	Department of Civil Engineering, Imperial College, 1995

[10]  	Eurocode 2: Design of concrete structures - Part 1-1: General rules and rules for buildings, ENV 1992-1:1991.

NSF Workshop on Structural Reliability in Bridge Engineering, Boulder, USA, October 1996.